

**CERTIFICATE OF ANALYSIS**

PRODUCT NAME : SILICA GEL 60-200 MESH

Code no. : SIL60-1K CAS no. : 112926-00-8

Lot no. : L185611601 Mfg date : JAN-2016

Exp date : DEC-2020 Analyzed on: 05/01/16

|  |  |  |  |
| --- | --- | --- | --- |
| Sr. no. | Tests | Specifications | Results |
| 1 | Description  | A white crystalline powder  | A white crystalline powder  |
| 2 | pH (10% slurry) | About 7.0 | 6.97 |
| 3 | Particle size | 60 - 200 mesh | Passes test |

This document has been produced electronically and it is valid without signature.